# Fevicol Product Range

Website copy for Fevicol SH, Marine, HiPer, and Pro Bond

# Fevicol SH

The Trusted Standard for Wood-to-Wood Bonding

India's No.1 carpentry adhesive — strong, reliable, everywhere.

## Overview

Fevicol SH is the adhesive that built India's carpentry industry. A premium-grade, polyvinyl acetate (PVA) based synthetic resin adhesive, it delivers a milky-white, ready-to-use emulsion that carpenters and furniture makers have trusted for generations. When you need a strong, dependable bond between wood and wood-based materials for everyday interior work, Fevicol SH is the adhesive that never lets you down.

Formulated for consistency and ease of use, Fevicol SH spreads smoothly, grips fast, and cures into a joint that's stronger than the wood around it. It's solvent-free, non-flammable, and free of any offensive odour — safe to use across the workshop, all day, every day.

## Key Features

- High bond strength — joints that outlast the furniture

- Fast handling strength: surfaces can be unclamped in 2–3 hours; full cure develops over 24 hours

- Smooth, easy application with brush or spatula — no mixing, no fuss

- Water-resistant (MR grade) for everyday indoor durability

- Solvent-free, non-flammable, and virtually odour-free

- Consistent milky-white emulsion, viscosity 200–300 Poise, for predictable spreading and grab

## Applications & Uses

- Carpentry and furniture-making — chairs, tables, cabinets, wardrobes, beds

- Bonding plywood, MDF, particle board, and hardboard to each other

- Laminate and veneer pasting onto wood-based panels

- General joinery and repair work in interior, dry environments

- Wood- and paper-based handicrafts and craft projects

## How to Apply

- Prepare: Ensure both surfaces are clean, dry, and free of dust, grease, or old adhesive residue.

- Apply: Spread a thin, even layer of Fevicol SH on one or both surfaces using a brush or spatula.

- Join: Press the surfaces firmly together, aligning them accurately before the adhesive begins to grab.

- Clamp: Hold under even pressure for 2–3 hours minimum; leave undisturbed for 24 hours for maximum bond strength.

- Clean: Wipe away any excess adhesive with a damp cloth before it dries.

## Specifications

| Appearance | Milky white emulsion |
| --- | --- |
| Viscosity (30°C) | 200–300 Poise |
| pH | 4–6 |
| Density (30°C) | 1.04–1.08 g/ml |
| Coverage | Approx. 45–50 sq. ft. per kg (at ~150 g/m²) |
| Handling time | 2–3 hours under pressure |
| Full cure | 24 hours |
| Water resistance | MR (Moisture Resistant) grade — for dry, interior use |
| Pack sizes | 50 g, 125 g, 250 g, 500 g, 1 kg, 2 kg, 5 kg, 10 kg, 20 kg, 30 kg, 50 kg |

## Frequently Asked Questions

Is Fevicol SH waterproof?

No. Fevicol SH is MR (Moisture Resistant) grade, suited to dry interior applications. For areas exposed to standing water or high humidity — kitchens, bathrooms, outdoor furniture — choose Fevicol Marine instead.

How long before I can use the bonded piece?

The joint can typically be unclamped after 2–3 hours, but for maximum strength, leave it under pressure for a full 24 hours before putting it under load.

Can Fevicol SH bond laminate to plywood?

Yes — it's widely used for pasting laminates and veneers onto plywood, MDF, and particle board for furniture and interior work.

What surfaces should I avoid using it on?

Fevicol SH is designed for wood-to-wood and wood-based panel bonding. It is not intended for PVC, acrylic sheet, metal, glass, or stone — for PVC/acrylic lamination, use Fevicol Pro Bond instead.

Which pack size is right for me?

Small packs (50 g–500 g) suit home repairs and small craft projects; 1–5 kg suits individual carpenters; 10 kg and above are built for workshops and bulk furniture production.

What is the shelf life of Fevicol SH, and how should I store it?

Like most Pidilite wood adhesives, Fevicol SH keeps well for around 2 years from manufacture when stored in a cool, dry place away from direct sunlight, with the container tightly sealed between uses. Always check the batch/manufacturing date on the pack, since shelf life can vary slightly by batch.

Can Fevicol SH be diluted with water?

A small amount of clean water (a few percent) can be added if the adhesive has thickened slightly, to bring it back to a workable consistency. Avoid over-diluting, as this weakens bond strength — for most jobs, use it straight from the pack.

Is Fevicol SH safe to use indoors?

Yes — it's solvent-free, non-flammable, and virtually odour-free, making it safe for regular indoor workshop use. As with any adhesive, avoid prolonged skin contact and wash hands after use; if it contacts eyes, flush with water.

How do I clean up excess or dried Fevicol SH?

Wipe excess adhesive with a damp cloth while it's still wet. Once dried, it can usually be gently scraped or sanded off; avoid harsh solvents on finished wood surfaces.

Can I paint or polish over a Fevicol SH joint?

Yes, once fully cured, the joint can be sanded flush and finished normally — just ensure all excess glue is cleaned off the surface before applying paint, polish, or laminate, as dried adhesive residue can affect finish absorption.

Why did my Fevicol SH joint fail?

Most joint failures come down to insufficient clamping time, applying too thin or too thick a layer, bonding dusty/oily surfaces, or exposing an MR-grade joint to sustained moisture. Following the prep, apply, and clamp steps closely resolves the vast majority of issues.

Does temperature affect how Fevicol SH performs?

Very cold conditions can slow curing, while very hot, dry conditions can cause the adhesive to skin over too quickly before you've joined the surfaces. Room temperature (roughly 20–30°C) gives the most predictable results.

Fevicol SH vs Fevicol HiPer — which should I pick for laminate work?

For standard laminates and everyday joinery, SH is the economical, reliable choice. If you're working with premium, thick laminates (1 mm+) or need faster handling strength to speed up production, HiPer is the better fit.

# Fevicol Marine

Genuine Waterproof Strength for Wet & Demanding Environments

When water is part of the job, Marine is the only adhesive built to win.

## Overview

Fevicol Marine is Pidilite's high-performance, BWP (Boiling Water Proof) grade adhesive — engineered for wood-based work that simply cannot afford to fail when moisture is involved. Where ordinary wood glue softens and lets go, Fevicol Marine holds firm through standing water, humidity, and repeated wet-dry cycles.

Beyond raw waterproofing, Fevicol Marine also resists fungal and bacterial growth, protecting bonded joints in permanently damp conditions — exactly the environments where furniture failure is most common and most costly.

## Key Features

- Genuine BWP grade: engineered to survive boiling water exposure, not just resist splashes

- Approximately 7 hours of boiling-water-proof protection and 7 days of normal water-proof protection

- Fast 4-hour setting time despite its heavy-duty formulation

- Resists fungus and bacteria — critical for permanently humid installations

- High bond strength that holds up under structural and environmental stress

- Formulated specifically for marine-grade and moisture-prone woodworking

## Applications & Uses

- Outdoor furniture exposed to rain and humidity

- Kitchen sink base units and bathroom vanity carcasses

- Window and door frames in wood

- Boats, docks, and other genuine marine/wet-area applications

- Any wood-to-wood or panel bonding where standing or flowing water is expected

## How to Apply

- Prepare: Use BWP/marine-grade plywood or substrate wherever possible — the adhesive can only protect the joint, not a substrate that isn't rated for water.

- Clean: Ensure surfaces are dry, clean, and free of grease or dust before application.

- Apply: Spread an even coat of Fevicol Marine on the mating surfaces.

- Join & Clamp: Press surfaces together and clamp firmly; initial set develops in about 4 hours.

- Cure: Allow a full cure period before exposing the joint to sustained water contact for best long-term performance.

## Specifications

| Grade | BWP (Boiling Water Proof) |
| --- | --- |
| Boiling water resistance | ~7 hours |
| Normal water resistance | ~7 days |
| Setting time | ~4 hours |
| Coverage | Approx. 34–38 sq. ft. per kg (double-side application) |
| Additional protection | Resists fungus and bacterial growth |
| Pack sizes | 1 kg, 5 kg, 10 kg, 20 kg, 50 kg and larger bulk quantities |

## Frequently Asked Questions

What does 'BWP grade' actually mean?

BWP stands for Boiling Water Proof — the highest water-resistance classification for wood adhesives, meaning the bond is engineered to withstand prolonged, even boiling, water exposure rather than just occasional dampness.

Is Fevicol Marine only for boats?

No — despite the name, it's used wherever wood meets water: outdoor furniture, kitchen and bathroom carcasses, window frames, and genuine marine applications alike.

Do I still need waterproof plywood if I use Fevicol Marine?

Yes. The adhesive protects the joint, but if the plywood itself isn't BWP/marine-grade, the wood can still be damaged by moisture even if the glue line holds. Pair Marine adhesive with marine-grade substrate for full protection.

How does it compare to Fevicol SH for a kitchen cabinet?

For dry interior cabinets, SH is sufficient and more economical. For anything near a sink, wet-prone kitchen base unit, or bathroom vanity, Marine is the safer, purpose-built choice.

How long should I wait before the piece gets wet?

Initial set is reached in about 4 hours, but allow the joint to cure fully before exposing it to sustained water contact for maximum durability.

What is the shelf life of Fevicol Marine, and how should I store it?

Store in a cool, dry place away from direct sunlight, with the lid tightly closed between uses — this preserves the adhesive's working consistency and waterproof performance. Check the manufacturing date on the pack, and use within roughly 2 years for best results.

Does Fevicol Marine resist fungus and mould, or just water?

Both. Beyond boiling-water resistance, it's formulated to resist fungal and bacterial growth, which matters in permanently damp joints where mould is often the real cause of long-term failure, not just water alone.

Is Fevicol Marine safe to use indoors?

Yes — used as directed, it's suitable for indoor workshop use. Avoid prolonged skin contact, ensure reasonable ventilation, and wash hands after use.

Can Fevicol Marine be used on outdoor furniture left in direct rain?

Yes, this is one of its core use cases — but for continuous outdoor exposure, also use weather-appropriate wood, finish the exposed surfaces well, and design joints to shed water rather than trap it.

Why did my 'waterproof' joint still fail?

The most common cause is pairing Marine adhesive with non-marine-grade plywood — the board itself absorbs water and swells even though the glue line holds. Insufficient clamping time or applying adhesive too thin can also weaken the bond.

Can I use Fevicol Marine for laminate and veneer pasting too?

Yes, it works for general wood-based bonding including laminates and veneers, but it's best reserved for pieces that genuinely need waterproof performance — for dry interior laminate work, Fevicol SH or HiPer is more economical.

How much Marine adhesive do I need for a sheet of plywood?

Coverage is approximately 34–38 sq. ft. per kg when applied to both surfaces — for a standard 8x4 ft plywood sheet (32 sq. ft.), budget roughly 1 kg per full-face bond, adjusting for panel size and overlap.

# Fevicol HiPer

High-Performance Speed for Premium Laminates & Veneers

Faster tack. Faster turnaround. Premium bonds, without the wait.

## Overview

Fevicol HiPer is a new-generation, high-strength adhesive purpose-built for premium, thick laminates (1 mm and above) and veneer pasting. Where standard wood glue takes its time, HiPer delivers a noticeably higher initial tack and faster handling strength — letting carpenters move to the next step of the job sooner without compromising on bond quality.

Designed for professionals who juggle tight deadlines and premium finishes in the same project, Fevicol HiPer is the adhesive of choice when speed and strength both matter.

## Key Features

- High initial tack for quick, confident positioning of laminates and veneers

- Handling strength develops in as little as 2 hours

- Engineered specifically for thick, premium-grade laminates (1 mm+)

- Strong, durable bond quality suited to professional furniture manufacturing

- Smooth application that reduces bubbling and lifting on large laminate sheets

## Applications & Uses

- Pasting premium and thick laminates onto plywood, MDF, and particle board

- Veneer bonding for high-end furniture and cabinetry

- Fast-turnaround carpentry projects and workshop production lines

- Furniture manufacturing where quick handling strength speeds up throughput

## How to Apply

- Prepare: Clean and dry both the substrate and the laminate/veneer surface thoroughly.

- Apply: Spread Fevicol HiPer evenly across both surfaces for a strong, uniform bond.

- Position quickly: Because of its high initial tack, align the laminate or veneer accurately before pressing — repositioning becomes difficult once contact is made.

- Press & Clamp: Apply firm, even pressure across the full surface, using a roller or clamps as appropriate for large panels.

- Hold: Maintain pressure until handling strength is reached (around 2 hours) before further processing.

## Specifications

| Ideal for | Premium laminates 1 mm and above, veneers |
| --- | --- |
| Handling strength | ~2 hours |
| Bond character | High initial tack, fast-setting |
| Pack sizes | 5 kg, 10 kg, 20 kg, 50 kg |

## Frequently Asked Questions

How is HiPer different from Fevicol SH?

Both are wood adhesives, but HiPer is formulated for faster initial tack and quicker handling strength — ideal when you're working with premium, thick laminates and can't afford long clamp times. SH is the general-purpose, budget-friendly choice for standard wood-to-wood joinery.

Is HiPer suitable for thin laminates?

It's specifically engineered for premium, thick laminates (1 mm and above) and veneers — for standard thin laminate work, Fevicol SH is typically sufficient.

Does the fast tack make it harder to reposition?

Yes — the higher initial tack that makes HiPer fast also means less time to adjust alignment. Position laminates and veneers accurately before pressing them into full contact.

How soon can I move the piece to the next process step?

Handling strength is reached in around 2 hours, letting workshops keep production moving without long downtime.

Is HiPer waterproof?

HiPer is built for speed and strength on laminate/veneer work, not for wet-area waterproofing. For moisture-heavy applications, use Fevicol Marine instead.

What's the shelf life of Fevicol HiPer, and how should it be stored?

Store in a cool, dry place away from direct sunlight with the container well sealed between uses — this keeps the adhesive's tack and viscosity consistent. As with other Fevicol wood adhesives, check the manufacturing date and use within roughly 2 years for best performance.

Can HiPer be applied with a roller for large laminate sheets?

Yes — for large panels, a notched trowel or roller helps achieve a fast, even coat across the full surface, which is important given how quickly the adhesive tacks up.

Why is my laminate bubbling after bonding with HiPer?

Bubbling usually points to an uneven adhesive layer, dust or debris trapped under the laminate, or insufficient pressure during pressing. Apply an even coat, press firmly from the centre outward, and use full-surface clamping or a roller for large sheets.

Is Fevicol HiPer suitable for a small home DIY project?

It can be, but its main advantage — speed — is most valuable in production settings. For a one-off home project without time pressure, Fevicol SH is simpler to work with and more forgiving of a slower pace.

Does HiPer need any special safety precautions?

No special precautions beyond standard adhesive handling — work in a reasonably ventilated space, avoid prolonged skin contact, and wash off any spills before they dry.

Can I mix HiPer and SH in the same project?

There's no harm in using both — many workshops use HiPer for premium laminate/veneer sections and SH for standard wood-to-wood joinery on the same piece of furniture, choosing whichever suits each specific bond.

# Fevicol Pro Bond

Specialist Adhesive for PVC & Acrylic Lamination

Built specifically for PVC and acrylic — where wood glue falls short.

## Overview

Fevicol Pro Bond is a water-based synthetic resin adhesive engineered specifically for laminating PVC and acrylic sheet onto MDF, plywood, and particle board. Standard wood adhesives aren't formulated to grip non-porous PVC and acrylic surfaces reliably — Pro Bond is. It's also the go-to choice for manual PVC edge-banding, letting carpenters apply PVC strips to board edges without an edge-banding machine.

GreenPro certified, Fevicol Pro Bond combines dependable adhesion with heat and moisture resistance, making it a natural fit for kitchens, wardrobes, and other interior spaces where PVC and acrylic finishes are increasingly popular.

## Key Features

- Purpose-built for PVC and acrylic sheet — not a generic wood glue repurposed for the job

- Enables manual PVC edge-banding without specialised machinery

- Bond strength develops in 4–6 hours; full strength within 24 hours at room temperature

- Heat and moisture resistant for kitchen and wardrobe applications

- Dries clear for a clean, professional finish

- GreenPro certified formulation

## Applications & Uses

- Laminating PVC sheet onto MDF, plywood, and particle board

- Bonding acrylic laminate to wood-based panels

- Manual edge-banding of PVC strips/tapes onto board edges

- Kitchen shutters, wardrobes, and furniture with PVC or acrylic finishes

## How to Apply

- Prepare: Ensure both the board surface and the PVC/acrylic sheet or strip are clean, dry, and dust-free.

- Apply: Spread Fevicol Pro Bond evenly on both surfaces to be joined.

- Wait for tack: Allow the adhesive to reach the right tack level as per pack instructions before joining, for the best bond on non-porous PVC/acrylic surfaces.

- Press: Join the surfaces and press firmly — for edge-banding, run firm, even pressure along the full length of the strip.

- Cure: Bond strength develops in 4–6 hours; allow 24 hours at room temperature for full strength before heavy handling.

## Specifications

| Best for | PVC sheet, acrylic laminate, PVC edge-banding strips/tapes |
| --- | --- |
| Appearance | Milky white emulsion |
| Viscosity (30°C) | 35–80 Poise |
| Bond strength time | 4–6 hours |
| Full strength | 24 hours at room temperature |
| Certification | GreenPro certified |
| Pack sizes | 500 g, 1 kg, 5 kg, 10 kg |

## Frequently Asked Questions

Can I use Fevicol SH instead of Pro Bond for PVC sheet?

No — Fevicol SH is formulated for wood-to-wood bonding and won't grip non-porous PVC or acrylic reliably. Pro Bond is purpose-built for these surfaces.

Do I need an edge-banding machine to use Pro Bond?

No — one of Pro Bond's key strengths is enabling manual PVC edge-banding, so small workshops can apply PVC strips without investing in machinery.

How long until the bonded panel can be handled normally?

Bond strength develops within 4–6 hours, with full strength reached at 24 hours at room temperature — avoid heavy handling before that.

Is Fevicol Pro Bond heat resistant?

Yes, it offers heat and moisture resistance suited to kitchen and wardrobe environments, though for extreme heat exposure near hobs, dedicated heat-resistant adhesives may be preferable.

What pack size should a small carpentry workshop start with?

500 g or 1 kg is ideal for testing and small jobs; 5 kg and 10 kg packs suit regular PVC/acrylic lamination work.

What is Fevicol Pro Bond's shelf life and how should it be stored?

Store in a cool, dry place away from direct sunlight with the lid tightly sealed between uses. As with other Fevicol wood-based adhesives, aim to use it within roughly 2 years of manufacture, and check the batch date on the pack.

Is Fevicol Pro Bond GreenPro certified — what does that mean for my project?

Yes, it's GreenPro certified, meaning it meets recognised sustainability and low-emission criteria — useful if you're marketing a project as eco-conscious or need to meet green-building material requirements.

Why isn't my PVC edge-banding strip sticking properly?

The most common causes are applying the adhesive too thick or too thin, not allowing it to reach the right tack before joining, dust or grease on the board edge, or insufficient pressure while pressing the strip down. Following the wait-for-tack step closely resolves most issues.

Can Pro Bond be used on wood-to-wood joints as well?

It's formulated and best suited for PVC and acrylic lamination. For standard wood-to-wood bonding, Fevicol SH or HiPer will give a stronger, more reliable result and is more cost-effective for that purpose.

Does Fevicol Pro Bond leave a visible glue line?

It dries clear, so with even application and proper pressing, the glue line is minimal and unobtrusive under PVC sheet or edge-banding strips.

Is Fevicol Pro Bond safe for kitchen use around food-prep areas?

It's designed for structural bonding within kitchen shutters and wardrobes (i.e., inside the panel construction), not as a food-contact surface. Once fully cured and sealed under the PVC/laminate finish, it poses no different handling concern than the panel itself.

What's the difference between Pro Bond and Fevicol Marine for a kitchen unit?

They solve different problems: Pro Bond bonds the PVC/acrylic finish to the board, while Marine is about waterproofing wood-to-wood joints. A kitchen unit with a PVC shutter in a wet-prone base area might use Pro Bond for the finish and Marine for the carcass joinery.